Thermodynamics

Stability of CONCENTRATED bitumen-salt-solvent mixtures 

N. Impens, P. Van Bree, J. Van Laer, P. Thomas, 

L. Vos, A. Fonteyne, S. Dekelver, R. Vandevoorde, Ann Leenaers

SCK•CEN, Mol, Belgium.

In the past, blown bitumen has been used as a matrix for inorganic radioactive waste such as (hydr)oxides or nitrate and sulphate salts of several metals, non-metals, transition metals and elements of the f-series. A weight ratio of 60:40 bitumen:waste was applied. The inorganic particles incorporated into the bitumen matrix are smaller than 40µm. During the production of this waste, bitumen (e.g. R85/40 from Shell), water and the inorganic particles were in close contact at 160°C in an extruder-evaporator. 

In the framework of studying the physicochemical interactions between the inorganic species and the bitumen matrix, we add an organic solvent to a home-made, non-radioactive simulated bitumen-waste mixture. As a function of the solubility parameter of the added solvent, different precipitates are formed. Elemental analysis of the precipitates as a function of the solubility parameter of the added solvent gives us a first idea on the physicochemical interaction of the inorganic species with the bitumen matrix. The same experiments are repeated with pure bitumen-solvent mixtures to study the effect of the salts on the (un)stability of the bitumen solution as a function of the solvent parameter. 

As dilution tremendously affects the thermodynamic behaviour of the simulated waste – solvent mixture, the tests are performed under conditions which are technically applicable if bituminised waste re-treatment by separation of the salts from the bitumen matrix would be necessary. We were able to study the (un)stability of highly concentrated bitumen-solvent and bitumen-salt-solvent mixtures using near infrared backscattering. 

